The files in this repository provide the raw data for all results described in this paper. The files are listed below with relevant comments.

| File name | Comment |
| --- | --- |
| 280311-4hr.raw | Bruker format data set for Rietveld, solid state reaction material |
| gem53596.gss | GEM GSAS data sets, solid state reaction material |
| si_103_gem52328.prm | Instrument parameter file for GEM data |
| 100983-mac-001_reb_005.xye | I11 data set, aqueous precursor route material |
| I11_Oct2011.ipf | Instrument parameter file for I11 data |
| 0d_HIPed_Cs2TiNb6O18.raw | Bruker data set, monolith, unleached |
| leached_28d_HIPed_Cs2TiNb6O18 | Bruker data set, monolith, leached 28 days |
| ExpDat_080911Cs2TiNb6O18-2 | TGA data, solid state route |
| ExpDat_080911cs2tinb6o18-2_m18_s1 | TGA data, aqueous route |
| 280311_Cs2TiNb6O18.ssd | XRF data, solid state route |
| Cs2TiNb6O18_solgel.ssd | XRF data, aqueous route |
| ICP_Report (091111).xls | ICP-MS data |